Shell Öl Absorption Granulat

Zur Aufnahme von Ölen, Fetten, Chemikalien, feuergefährlichen und brennbaren Flüssigkeiten

Das Öl Absorptions Granulat ist ein Micro-Aufsaugmittel, vollständig auf Calcium- Basis. Es ist nicht schmierend und ist speziell für rauhe und glatte Böden.

Das Produkt erfüllt die strenge Deutsche Norm Typ III R von der MPA-NRW (Materialprüfungsamt NRW) für stark verölte Oberflächen.

Produktinformationen:

Granulometrie

Dichte	519 kg/m≥	> 10 MESH	0%

Absorption 		> 18 MESH	45%

Westinghouse water (Aufsaugkapazität)	127 %	< 50 MESH	0,3 %

Westinghouse Öl (Aufsaugkapazität)	86 % 	staubarm

Granulatgrösse:	0,3 – 1 mm	< 0,125	0,5

Zusammenstellung:

SiO2 (74%), Al2O3 (11%), Fe2O3/FeO (7%), MgO (2%), K2O (1,5%), TiO2 (1%), CaO (1%), Na2O (0,5%) Ignition Loss (2%), ph Wert: 5-8

Eigenschaften:

Das Granulat beinhaltet keine gefährlichen Stoffe und ist aus Calciumnitrat gefertigt.

Es ist ungefährlich für Mensch und Umwelt, und ist in reiner Form angewendet keine Gefahr für das ökologische System. Es ist nicht brennbar und beständig gegen alle Chemikalien, außer Hydrofluorid Säure.

Für dieses Absorptions Granulat ist keine Kennzeichnung vorgeschrieben.

Anpassungsliste für:

Acetaldehyde 	Chlorobenzene 		Hydrozine	Propanol

Acetic Acid  	Chloroform 	Hydrochloric Acid 	Propionic Acid

Acetic Anhydride	Chromic Acid (50 %) 	Hydrofluoric Acid 	Propyl Alcohol

Acetone	Chlorosultonic Acid 	Hydrogen Cyanide 	Propylene Glycol

Acetyl Chloride 	Citric Acid 	Hydrogen Peroxide 	Quinoline

Acrolein 	Clorox (Full Strenght Bleach) 	Isobutyl Alcohol 	Resorcinol

Acrylanitrile 	Corn Oil 	Isobutric Acid 	Salt Solutions (metalic}

Acrylic Acid 	Cotton Seed 	Isopropyl Acetate 	Silicone Oil

Acrylic Emulsions 	Creosol 	Isopropyl Alcohol 	Silver Nitrate

Allyl Alcohol 	Cutting 	Kerosene 	Soap Solutions

Aminobenzoic Acid 	Cyclahexane 	Keytones 	(concentrated)

Ammonia (Anhydrous)	Detergents 	Linseed Oil 	Sodium Bicarbonate

Ammonium Hydroxide 	Dichlorobenzene 	Lubricating Oil 	Sodium Chloride

Amyl Acetate 	Diethylamine 	Magnesium Hydroxide 	Sodium Hyclroxide.

Aniline 	Diethyl Ether 	Methyl Alcohol 	Sodium Hypochlorite

Aqua Regina 	Disaoctyl Phthalate 	Methyl Chloride 	Sodium Nitrate

Aviation Fuel 	Dinitrobenzene 	Methyl Ether 	Stannic Chloride `

Benzene 	Dioxan Methyl 	Ethyl Ketone 	Starch

Benzoic Acid 	EDM Oils 	Methyl Propionate 	Styrene

Benzonitrile 	Ether 	Mineral Oil 	Sucrose

Benzoyl Chloride 	Ethyl Acetate 	Motor Oil 	Sulturic Acid Q

Benzyl Alcohol 	Ethyl Alcohol 	Napthalene Synthetic 	Motor`Oil

Boric Acid 	Ethyl Benzene 	Nitric Acid 	Tannic Acid

Brake Fluid 	Ethyl Chloride 	Nitrobenzene 	Toluene `

Bromine Ethyl 	Ether 	Nitrobenzoic Acid 	Transformer Oil

Butyl Acetate 	Ethyl Propioate 	Nitrotoluene 	Trichlorethylene

Butyl Alcohol 	Ethylene Glycol 	Octane 	Triethylene Glycol

Butyric Acid 	Formaldehyde 	Oleic Acid 	Turpentine

Butylamine 	Formic Acid 	Olive Oil 	Urine

Calcium Hydroxide 	Fuel Oil 	Parafin ·	Vinyl Acetate

Carbolic Acide 	Gasoline 	Perchloroethylene   	Vinegar

Carbon Disullide 	Gearbox Oil 	Petroleum Ether 	Water Soluble Cutting Oils

Carbon Tetrachloride 	Glacial Acetic Acid 	Phenol 	Xylene

Castor Oil, 	Glycerol 	Phosphoric Acid

Chlorine Water 	Heptane 	Plating Solutions

Chloroacetic Acid 	Hexane 	Potasium Hydroxide