Shell Omala HD

Synthetic heavy duty industrial gear oils

Shell Omala HD is an advanced synthetic heavy duty industrial gear oil offering outstanding lubrication performance under severe operating conditions, including improved energy efficiency, long service life and high resistance to micro-pitting for optimal gear protection

Applications

Enclosed industrial reduction gear systems operating under severe operating conditions, such as high load, very low or elevated temperatures and wide temperature variations

Particularly recommended for certain ‘lubricated-for-life’ systems

Plain and rolling element bearings

Oil circulation systems

Performance Features and Benefits

Excellent load carrying capacity and micro-pitting performance providing long component life

Provides high levels of load carrying capacity even under shock loading conditions, along with high resistance to micro-pitting (grey staining).  These features provide benefits over mineral oil-based products in terms of gear and bearing component life.

Excellent oxidation and thermal stability extending lubricant life

Resists the formation of harmful products of oxidation at high operating temperatures, improving system cleanliness and therefore reliability of the equipment.  Omala HD is formally approved by Flender AG for at least 20,000 operating hours or four years, assuming an average operating temperature of 80 °C.

Omala HD can operate successfully at

bulk operating temperatures of up to 120°C.

Longer service intervals

Extended component and lubricant life offers the opportunity to extend service intervals and to reduce maintenance and disposal costs.

Superior lubricant performance improving gear efficiency

Offers improved low temperature performance and reduced change in viscosity with increase in temperature in comparison to mineral oil-based products.  This provides better lubrication at low start-up temperatures and the opportunity for energy savings by optimising the viscosity for normal operating conditions.

Outstanding rust and corrosion protection of all metal surfaces

Rapid water shedding and air release performance

Specifications and Approvals

Meets ISO 12925-1 Type CKD

Meets ANSI/AGMA 9005-D94

Meets US Steel 224

Fully approved by Flender AG

Meets David Brown S1.53.101

Meets the requirements of DIN 51517-3

Seal and paint compatibility

Omala HD is compatible with all seal materials and paints normally specified for use with mineral oils.

Change over procedure

Omala HD is based on synthesized hydrocarbon fluids and is compatible with petroleum mineral oils - no special change-over procedure is necessary.  However, to achieve the complete benefit of Omala HD they should not be mixed with other oils.

It is also advisable to ensure that oil systems are clean and free from contamination.

Advice

Advice on applications not covered in this leaflet may be obtained from your Shell representative.

Health and Safety

Guidance on Health and Safety are available on the appropriate Material Safety Data Sheet, which can be obtained from your Shell representative.

Protect the environment

Take used oil to an authorized collection point.  Do not discharge into drains, soil or water.

Typical Physical Characteristics

|  | Omala HD |  |  |  | 68 | 100 | 150 | 220 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ISO Viscosity Grade |  |  | ISO 3448 | 68 | 100 | 150 | 220 |
|  | Kinematic Viscosity |  |  | ISO 3104 |  |  |  |  |
|  |  | at 40°C | mm2/s |  |  | 69.3 | 101.8 | 157.7 | 229.4 |
|  |  | at 100°C | mm2/s |  |  | 11.4 | 15.5 | 21.7 | 28.3 |
|  | Viscosity Index |  |  | ISO 2909 | 158 | 161 | 163 | 160 |
|  | Flash Point COC | °C |  | ISO 2592 | 228 | 232 | 238 | 250 |
|  | Pour Point | °C |  | ISO 3016 | -54 | -51 | -45 | -45 |
|  | Density at 15°C | kg/m3 |  | ISO 12185 | 861 | 873 | 877 | 881 |
|  | FZG Load Carrying Test |  |  | DIN 51354-2 |  |  |  |  |
| Failure load stage |
|  | A/8.3/90 | >12 | >12 | >12 | >12 |
|  | Timken OK Load | lbs |  | ASTM D 2782 | >85 | >85 | >85 | >85 |
|  |  | Omala HD |  |  |  | 320 | 460 | 680 | 1000 |
|  | ISO Viscosity Grade |  |  | ISO 3448 | 320 | 460 | 680 | 1000 |
|  | Kinematic Viscosity |  |  | ISO 3104 |  |  |  |  |
|  |  | at 40°C | mm2/s |  |  | 312.7 | 462.6 | 670.4 | 1002 |
|  |  | at 100°C | mm2/s |  |  | 35.4 | 50.0 | 64.9 | 94.4 |
|  | Viscosity Index |  |  | ISO 2909 | 159 | 170 | 169 | 183 |
|  | Flash Point COC | °C |  | ISO 2592 | 252 | 264 | 256 | 260 |
|  | Pour Point | °C |  | ISO 3016 | -42 | -36 | -33 | -24 |
|  | Density at 15°C | kg/m3 |  | ISO 12185 | 883 | 879 | 881 | 901 |
|  | FZG Load Carrying Test |
|  | DIN 51354-2 |  |  |  |  |
| Failure load stage |
|  | A/8.3/90 | >12 | >12 | >12 | >12 |
|  | Timken OK Load | lbs |  | ASTM D 2782 | >90 | >90 | >90 | >90 |

These characteristics are typical of current production.  Whilst future production will conform

to Shell's specification, variations in these characteristics may occur.